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SECTION 11 66 10
SPORTS NETTING
GENERAL
SECTION INCLUDES
 Provide and install athletic netting as indicated on the drawings and specified herein, including but not limited to:
Baseball/softball netting.
Golf netting.
SUBMITTALS
Product Data: Submit manufacturer's product data prior to field installation work, for Architects or Owners representatives review.
Samples:  If requested, submit three representative samples of each type and size of netting required.
QUALITY ASSURANCE
Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum of five years documented experience.
DELIVERY, STORAGE, AND HANDLING
Examine materials for upon delivery for damage or defects. Report any deficiencies to the Owner’s representative and promptly replace damaged or defective materials to avoid impact to the construction schedule. 
Store and handle materials above ground, protected from weather, and stored under cover or indoors until installation.
WARRANTY
0. Manufacturers standard warranties shall pass to the Owner. Provide Certification that materials furnished comply with applicable industry standards, quality requirements, and manufacturer’s published product data.
PRODUCTS
MANUFACTURER
Manufacturer:  On Deck Sports, Randolph, MA Tel 800.365.6171 www.ondecksports.com bids@ondecksports.com
#36-Gauge Baseball/Softball Netting by On Deck Sports:
Mesh:  1-3/4 inch square-hung mesh
Yarn Type:  #36-gauge knotted nylon with UV protection.
Rope Border: 1/4 inch braided sewn rope border.
Tensile Strength:  325 pounds.
Finish:  Bonded.
Color:  Black.
#42-Gauge Baseball/Softball Netting by On Deck Sports:
Mesh:  1-3/4 inch square-hung mesh
Yarn Type:  #42-gauge knotted nylon with UV protection.
Rope Border: 1/4 inch braided sewn rope border.
Tensile Strength:  370 pounds.
Finish: Bonded.
Color:  Black.
#60-Gauge Baseball/Softball Netting by On Deck Sports:
Mesh:  1-3/4 inch square-hung mesh
Yarn Type:  #60 knotted nylon with UV protection.
Rope Border: 1/4 inch braided sewn rope border.
Tensile Strength:  551 pounds.
Finish:  Bonded.
Color:  Black.
#18-Gauge Golf Barrier and Protective Netting by On Deck Sports:
Mesh:  7/8 inch square-hung mesh
Yarn Type:  #18-gauge knotted nylon with UV protection.
Rope Border: 1/4 inch braided sewn rope border.
Tensile Strength:  154 pounds.
Finish:  Bonded.
Color:  Black
EXECUTION
EXAMINATION
Examine substrates, areas, and conditions, with Installer present, to verify conditions affecting performance of work.  Proceed with installation only after unsatisfactory conditions have been corrected.
INSTALLATION
Install netting in accordance with manufacturer’s instructions, approved submittals, and in proper relationship with adjacent construction.
Repair or replace components damaged during installation.
Clean exposed surfaces using methods acceptable to the manufacturer.
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